| Type of distress | Severity Level | Treatment |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Full-depth crack repair | Clean and seal | Saw and seal | Rout and seal | Crack filling | Patching | Chip seal or seal coat | Thin hot mix overlay | Fog seal | Seal coat | Double chip seal | Slurry seal | Micro-surfacing |
| Cracking: Alligator or Fatigue | Low |  |  |  |  |  |  | X |  |  |  |  |  |  |
|  | Moderate |  |  |  |  |  | X |  |  |  |  |  |  |  |
|  | High |  |  |  |  |  | X |  |  |  |  |  |  |  |
| Cracking: Transverse | Low |  | X |  | X |  |  | X |  |  |  |  |  |  |
|  | Moderate |  | X |  | X | X |  | X |  |  |  |  |  |  |
|  | High | X |  |  |  | X | X | X |  |  |  |  |  |  |
| Cracking: Longitudinal | Low |  | X |  | X | X |  |  |  |  |  |  |  |  |
|  | Moderate | X | X |  | X | X |  |  |  |  |  |  |  |  |
|  | High | X |  |  |  | X | X |  |  |  |  |  |  |  |
| Cracking: Block | Low |  | X |  | X |  |  | X |  |  |  |  |  |  |
|  | Moderate |  |  |  |  |  |  | X | X |  |  |  |  |  |
|  | High |  |  |  |  | X | X |  | X |  |  |  |  |  |
| Cracking at joints: Reflection | Low |  | X |  | X |  |  |  |  |  |  |  |  |  |
|  | Moderate |  | X |  | X | X |  |  |  |  |  |  |  |  |
|  | High |  | X |  |  | X | X |  | X |  |  |  |  |  |
| Potholes | Low |  |  |  |  |  | X |  |  |  |  |  |  |  |
|  | Moderate |  |  |  |  |  | X |  |  |  |  |  |  |  |
|  | High |  |  |  |  |  | X |  |  |  |  |  |  |  |
| Patch deterioration | Low |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Moderate |  |  |  |  |  | X |  |  |  |  |  |  |  |
|  | High |  |  |  |  |  | X |  |  |  |  |  |  |  |
| Rutting | Low |  |  |  |  |  | X |  |  |  |  |  | X | X |
|  | Moderate |  |  |  |  |  | X |  | X |  |  |  | X | X |
|  | High |  |  |  |  |  | X |  | X |  |  |  |  | X |
| Shoving | Low |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Moderate |  |  |  |  |  | X |  |  |  |  |  |  |  |
|  | High |  |  |  |  |  | X |  |  |  |  |  |  |  |
| Bleeding | Low |  |  |  |  |  |  |  |  |  | X | X | X | X |
|  | Moderate |  |  |  |  |  |  |  |  |  | X | X | X | X |
|  | High |  |  |  |  |  |  |  | X |  | X | X | X | X |
| Polished Aggregate | Low |  |  |  |  |  |  |  |  |  | X | X | X | X |
|  | Moderate |  |  |  |  |  |  |  | X |  | X | X | X | X |
|  | High |  |  |  |  |  |  |  | X |  | X | X | X | X |
| Raveling | Low |  |  |  |  |  |  |  |  | X |  |  |  |  |
|  | Moderate |  |  |  |  |  |  |  |  | X | X |  |  |  |
|  | High |  |  |  |  |  | X |  | X |  | X | X | X | X |